Conbextra EP935

**A free flowing, water displacing epoxy grout for underwater grouting applications**

**1.0 Grouting Requirements**

* 1. To the nominated area(s) (specify details and areas of application), grouting must be carried out using an epoxy resin grout, suitable for application under water.
  2. The two-component pack is to be stored, handled and placed, strictly in accordance with the manufacturer’s current technical data sheet and instructions. The grout should be installed by a suitably experienced contractor.
  3. The hardened epoxy resin grout shall exhibit the following properties at 23oC:

|  |  |
| --- | --- |
| Compressive strength: | 50 MPa @ 1 day |
| 90 MPa @ 7 days |
| Specific gravity | 2.0 |
| Pot life: | 60 mins. @ 20oC (1kg mix) |

* 1. **Fosroc Conbextra EP935** meets the performance criteria and is approved for this application