Proofex® PGP

PVC waterproof membrane

1.00	PVC Sheet Waterproofing

Where so designated on the drawings, the waterproof membrane shall be flexible PVC suitable for 	application as a loose laid or fully bonded system for waterproofing tunnels and other below ground 	structures.

1.10	Surface Preparation

Surfaces should be free from cavities and projecting nibs. All surfaces shall be free from running water.

1.20	Waterproofing Membrane

The waterproofing membrane is to be a 2mm thick PVC sheet, coloured light grey on top and black on 	the underside to help identify any damages that may occur during application.

It shall exhibit the following properties:

| Tensile Strength sheet only (EN 12311-2): | Transverse: >14 N/mm2 Longitudinal: >16 N/mm2 |
| --- | --- |
| Cold flexibility (EN495-5 @ -35OC): | Pass |
| Elongation at Break (EN12311-2): | Transverse: >300% Longitudinal: >300% |
| Tear resistance (EN 12310-1): | >340 N |
| Puncture resistance (ASTM E154-08): | 1200 N |
| Water Impermeability (EN 1928): | Pass |
| Water vapor transmission (ASTM E96): | Nil |
| Lap joint strength (EN12317 and UEATc): | >1000 N/50mm (broken out joint) |
| Root resistance (EN TS14416): | Pass – no penetration |

.

1.21	The waterproofing membrane shall be applied in accordance with the manufacturer’s product data 	sheet.

1.30	Fosroc Proofex PGP meets the performance criteria and is approved

Mar-07

Mar-07

.